Title
Why do we need trap states when simulating disordered devices?
[alternative title: Please stop simulating disordered semiconductors without trap states]
Dr. Roderick MacKenzie
roderick.mackenzie@oghma-nano.com
Winter 2022
https://www.oghma-nano.com

---
Overview
Introduction
Standard drift diffusion models for ordered materials such as GaAs
Comparison of disordered and ordered semiconductors
Why is having the correct distribution of trap states important?
Furthermore… mobility…
Simulating disordered devices with traps
Including the SRH equation is not enough esp in time domain.
Demos

---
Why am writing this slide deck on a weekend?
Recently I’ve noticed a few ‘drift diffusion’ models being applied to disordered materials without trap states.
Broadly speaking this should not be done, so I thought I would make some comments as to why this should not be done.

---
Some examples

---
Some examples

---
Second paper
Monte-Carlo hopping with traps
Drift diffusion model with no traps
size 20 {nabla %epsilon_o %epsilon_r cdot nabla %phi = q cdot (n-p)}
size 20 {J_n=q %mu_e n nabla E_c + q D_n nabla n}
size 20 {J_p=q %mu_h p nabla E_v - q D_p nabla p}
They concluded that you need traps and their DD model did not work as it had no traps.
Picture from:10.1038/srep19794
I broadly agreed with their conclusion but I think they should not have been modeling disordered devices without traps in the first place.

---
Overview
Introduction
Standard drift diffusion models for ordered materials such as GaAs
Comparison of disordered and ordered semiconductors
Why is having the correct distribution of trap states important?
Furthermore… mobility…
Simulating disordered devices with traps
Including the SRH equation is not enough esp in time domain.
Demos

---
An ordered semiconductor such as GaAs
Ec
μe
Electron
Majority
contact
Ev
μh
Hole
Majority
contact
Electron energy

---
Simulating charge transport for ordered semiconductors.
Gauss's Law
size 20 {nabla %epsilon_o %epsilon_r cdot nabla %phi = q cdot (n-p)}
Electron driving terms
Hole driving terms
size 20 {J_n=q %mu_e n nabla E_c + q D_n nabla n}
size 20 {J_p=q %mu_h p nabla E_v - q D_p nabla p}
Hole continuity
Electron continuity
size 20 {nabla cdot {bold J}_p = -q left ( R_p +T_p + {partial p_{free}} over {partial t} right )}
size 20 {nabla cdot {bold J}_n = q left ({R_n+T_n+ {partial n_{free}} over {partial t}} right )}
Demo
MacKenzie , Shuttle, Adv. Energy Mater. 2012, 2 (6), 662-669

---
Overview
Introduction
Standard drift diffusion models for ordered materials such as GaAs
Comparison of disordered and ordered semiconductors
Why is having the correct distribution of trap states important?
Furthermore… mobility…
Simulating disordered devices with traps
Including the SRH equation is not enough esp in time domain.
Demos

---
Compare band structure of silicon and
an organic semiconductor
Inorganic semiconductors are crystalline and have a well defined bandgap and few traps.
Inorganic semiconductors are very disordered and have a distribution of trap states.
Conduction band
Band gap – No carriers
Valance band
Conduction band
Valance band
Electron energy
Photon
Electron energy
Photon

---
The majority of charge is stored in these trap
states
Conduction band
Electron energy

---
So this type of model is not valid as there are no traps
Ec
Electron
Majority
contact
Ev
Hole
Majority
contact
Electron energy

---
We need to add carrier traps to our model
Ec (LUMO)
Electron
Majority
contact
Carrier traps
Carrier traps
Ev (HOMO)
Hole
Majority
contact
Electron energy

---
Then it starts to look a lot more like the traditional Monte-Carlo hopping models.
Ec (LUMO)
Electron
Majority
contact
Carrier traps
Carrier traps
Ev (HOMO)
Hole
Majority
contact
Picture from:10.1038/srep19794
Electron energy

---
Overview
Introduction
Standard drift diffusion models for ordered materials such as GaAs
Comparison of disordered and ordered semiconductors
Why is having the correct distribution of trap states important?
Furthermore… mobility…
Simulating disordered devices with traps
Including the SRH equation is not enough esp in time domain.
Demos

---
The trap distribution determines the voltage and light dependence of carrier density.
In disordered devices because all the charge is stored in trap states, carrier density in the device varies strongly as a function of applied voltage and light intensity
n(V,light), p(V,light)

---
The trap distribution determines the voltage and light dependence of carrier density.
Or said in another way rho (the DoS) multiplied by the fermi level determines charge density.
n
p
OK so what you might ask?

---
Recombination is a strong function of carrier density.
R=f(n(V,light),p(V,light))
So to get recombination correct we need to get n(V,light) and p(V,light) correct.
Note the very simplified recombination model, don’t assume
your material is bi-molecular but that is another story.

---
Getting recombination correct is key to getting Jsc, Voc, and FF correct.

---
Overview
Introduction
Standard drift diffusion models for ordered materials such as GaAs
Comparison of disordered and ordered semiconductors
Why is having the correct distribution of trap states important?
Furthermore… mobility…
Simulating disordered devices with traps
Including the SRH equation is not enough esp in time domain.
Demos

---
Mobility in ordered materials is constant
size 20 {J_n=q %mu_e n nabla E_c + q D_n nabla n}
Ec
μe
Electron
Majority
contact
Ev
μh
Hole
Majority
contact
size 20 {J_p=q %mu_h p nabla E_v - q D_p nabla p}
Electron energy

---
In disordered material it’s not constant, imagine the following situation:
All our carriers have lots of energy and are free:
μ=μe
Electron
Majority
contact
Carrier traps
μ=0
Hole
Majority
contact
What’s the mobility? …… μe
Electron energy

---
In disordered material it’s not constant, imagine the following situation:
All our carriers are trapped:
μ=μe
Electron
Majority
contact
μ=0
Hole
Majority
contact
What’s the mobility? ….. 0
Electron energy

---
In general….
When some carriers are free and some are trapped..
μ=μe
Electron
Majority
contact
μ=0
Hole
Majority
contact
size 30 {%mu = {n_{free} %mu_e } over {n_{free}+n_{trap}} }
So if you get ntrap wrong you will have the wrong dependence of mobility on voltage, light which will also cause problems for your model..
Electron energy

---
Overview
Introduction
Standard drift diffusion models for ordered materials such as GaAs
Comparison of disordered and ordered semiconductors
Why is having the correct distribution of trap states important?
Furthermore… mobility…
Simulating disordered devices with traps
Including the SRH equation is not enough esp in time domain.
Demos

---
Let’s slice through the device in energy space
LUMO
Carrier traps
Metal
contact
Carrier traps
Transparent
contact
HOMO
Electron energy

---
We therefore need to solve for the charge density of each trap state explicitly.
We split energy space up into energy slices.
And use the SRH equations but don’t assume steady state, so solve the SRH equations explicitly in time domain.
Each trap state gets its own rate equation:
Recombination can be calculated as:
Free carrier recombination
size 20 {R_n = sum from 0 to n_{band} (r^e_1-r^e_2)}
size 20 {{partial n} over {partial t}= r_1 -r_2 -r_3 +r_4}
Detailed balance
is maintained.
Process
electron capture
size 16 {r_1}
size 16 {r_2}
electron emission
hole capture
size 16 {r_3}
size 16 {r_4}
hole emission

---
SRH recombination and trapping model.

---
This enables us to know where the charge carriers are in position/energy space.
LUMO mobility edge
LUMO traps
HOMO traps
HOMO mobility edge
Carrier density m-3

---
Overview
Introduction
Standard drift diffusion models for ordered materials such as GaAs
Comparison of disordered and ordered semiconductors
Why is having the correct distribution of trap states important?
Furthermore… mobility…
Simulating disordered devices with traps
Including the SRH equation is not enough esp in time domain.
Demos

---
Steady state SRH v.s. fully time/spatially resolved SRH.

---
Steady state SRH v.s. fully time/spatially resolved SRH.
Using the steady state SRH approach acknowledges that carrier traps are important in recombination.
You won’t get the correct carrier density voltage dependence in the device.
And the charge in the trap states is not linked back to the electrostatic potential.
But it assumes the distribution of trap states has reached equilibrium. This is OK for steady state but not for time domain.
It also fails to take into account the distribution of trap states.